# Thermal Properties of Matter

| Specific Heat Substance J/kg°C Aluminum 900 Copper 387 Germanium 322 Glass 837 Gold 129 Ice 2090 Iron 448 Lead 128 Mercury 138 Silicon 703 Silver 234 Steam 2010 Water 4186 | Linear Expansion Material Coefficient (C-1) Aluminum 2.40 x 10-5 Brass and Bronze 1.90 x 10-5 Copper 1.70 x 10-5 Glass (ordinary) 9.00 x 10-6 Glass (Pyrex) 3.20 x 10-6 Lead 2.90 x 10-5 Steel 1.10 x 10-5 Invar (Ni-Fe alloy) 9.00 x 10-7 Concrete 1.20 x 10-5 |
| --- | --- |
| Latent Heats of Fusion and Vaporization Substance Melting Point (C) Latent Heat of Fusion (J/kg) Boiling pt (C) Latent Heat Of Vaporization (J/kg) Helium -269.65 5.23 x 103 -268.93 2.09 x 104 Nitrogen -209.97 2.55 x 104 -195.81 2.01 x 105 Oxygen -218.79 1.38 x 104 -182.97 2.13 x 105 Ethyl alcohol -114.00 1.04 x 105 78.00 8.54 x 105 Water 0.00 3.33 x 105 100.00 2.26 x 106 Lead 327.30 2.45 x 104 1750.00 8.70 x 105 Aluminum 660.00 3.97 x 105 2450.00 1.14 x 107 Silver 960.80 8.82 x 104 2193.00 2.33 x 106 Gold 1063.00 6.44 x 104 2660.00 1.58 x 106 Copper 1083.00 1.34 x 105 1187.00 5.06 x 106 |